## Slide 1: Overview of Target Initiatives for the First Target Station
Mark Wendel
Acting Group Leader,
Source Development and Engineering
SNS Accelerator Advisory Committee Meeting
February 16–18, 2016

## Slide 2: Contents
History of targets and leaks
Recent happenings since 2014 leaks
Goals for reliability
Initiatives to reach the goals
  Benefit
  Highlight
  Development
Summary

## Slide 3: T13 is now in service, capable of handling the SNS nominal power of 1.4 MW
23 kJ/pulse at 1.4 MW
700 ns pulse, 60 Hz
5 x 106 pulses/day
Proton beam
1.3 m
Notes: The target module is not a safety credited component.
We do thorough engineering to assure reliable service to account for what is known.
Acknowledging that a first of a kind component like this has uncertainties, not safety crediting it is prudent.

## Slide 4: Target change-outs for SNS (13 targets in 10 years)
T1
T2
T3
T4
T5
T6
T7
T8
T9
T10
T11
T12
T13
[Baumgartner, Target Breakout]

## Slide 5: The targets that failed early came in pairs
Target | Exposure (MW-hrs) | Avg. Power (KW) | Failure
 | 3055 | 379 | None (Removed from Service)
 | 3145 | 771 | None (Removed from Service)
 | 2791 | 845 | Unknown
 | 3252 | 782 | None (Removed from Service)
 | 2362 | 938 | None (Removed from Service)
 | 617 | 916 | Transition cover plate weld
 | 98 | 943 | Transition cover plate weld
 | 3750 | 851 | None (Removed from Service)
 | 4195 | 1033 | None (Removed from Service)
 | 601 | 1052 | Front / transition weld
 | 167 | 1116 | Transition cover plate weld
 | 4445 | 964 | TBD – leaked on nose
 | 1565 | 1000 | In service
1
2
3
6
7
9
8
4
5
10
11
12
13
x
Original target
Jet-flow target
x
x
Original target plus
2012
Fabrication Improvements
2014
Design Improvements

## Slide 6: For the nineteen target modules that have been manufactured…
Six have been operated and removed from service with no indication of a leak
Six have been operated and removed from service due to a mercury leak
  Four leaked early (< 617 MW-hr)
  Two leaked later (2791 and 4445 MW-hr)
Six have not yet been used
  Two are on site
  Four are at some stage of fabrication
One is in service now (>1500 MW-hr)

## Slide 7: Inventory projection indicates that another order should be placed soon in order to remain 4 targets deep
Winter 15/16 Shutdown | Early 16 | Summer 16 Shutdown | Late 16 | Winter 16/17 Shutdown (IRP) | Early 17 | Summer 17 Shutdown | Late 17 | Winter 17/18 Shutdown | Early 18 | Summer 18 Shutdown | Late 18 | Winter 18/19 Shutdown | Early 19
 | MTX-009 |  | MTX-010 |  | MTX-011 |  | MTX-011 |  | MTX-013 |  | MTX-012 |  | MTX-008
 | ORTE-003 |  | ORTE-003 |  | ORTE-003 |  | ORTE-003 |  | ORTE-003 |  | ORTE-003 |  | ORTE-003
 | MTX-010 |  | MTX-013 |  | MTX-013 |  | MTX-013 |  | MTX-012 |  | MTX-008 |  | 
 |  |  | MTX-011 |  | MTX-012 |  | MTX-012 |  | MTX-008 |  |  |  | 
 |  |  | MTX-012 |  | MTX-008 |  | MTX-008 |  |  |  |  |  | 
Installed
Ready Spares
Arriving Spares
Lead time for a new target is typically 18 months
[Winder, Target Breakout]

## Slide 8: We have identified the leak locations for all but one of the 6 targets that leaked
T6, T7, T11 Leak (early/weld)
T12 Leak (very late)
T3 Leak – late/undetermined
T10 Leak – Jet-flow target (early/weld)

## Slide 9: DOE Office of Science Independent Review conducted for Feb. 24-25, 2015
Almost all recommendations by committee were accepted
  Significant progress already made on most recommendations
  Vibration diagnostic and weld-annealing were considered but not implemented
Target development funding was provided
Target initiatives were organized
Still continuing weekly meetings to track progress

## Slide 10: Also, since the Feb 2015 review…
Strategic goals have been set for SNS targets
  1.4 MW operation
  No more than 2 target changes per year
  Predictable target change-outs
STS CD1 effort has been funded
  FTS expected to receive 2 MW, requiring more robust target design
  Need to evaluate FTS for power exceeding 2 MW
Two more targets have been operated
  Target T12 set longevity record at 4445 MW-hr
  Target T13 is still operational at 1567 MW-hr

## Slide 11: Progress toward goal of 1.4-MW reliable operation with ≤ 2 changes per year
Operated 4 targets between 1.3 – 1.4 MW
  T8 for 1 cumulative-day* (no leak)
  T9 for 15 cumulative-days (no leak)
  T12 for 25 cumulative-days before a leak
  T13 for 15 cumulative-days and still going (no leak yet)
T9 was operated
  6 months above 1 MW
  3 months above 1.2 MW
  did not leak mercury
New “improved” designs are on their way
  T13 (in service) already has several improvements over T12
  T14 has even more improvements
*for 6-months of time, there are 104 cumulative-days of operation based on a 5000-hr year

## Slide 12: Engineering challenges to target design & build must be addressed
Multiple failure modes interact through non-linear relationships
  Beam-induced cavitation
  High-cycle fatigue
  Corrosive/erosive actions of mercury
Cannot approach the 1.4 MW goal slowly
Long lead times
  A minimum of two years is required to respond to any issue that is identified
    Post-irradiation examination (PIE)
    Design and analysis
    Fabrication
There is no encompassing design criteria … yet!

## Slide 13: Current initiatives should help reach both short and long term performance goals
Re-design of the targets
Hg vessel strain measurements during SNS beam
Fabrication improvements
Gas injection
Increase the pump speed
Improve PIE capabilities

## Slide 14: Re-design of the targets
Benefit: Structure is robust to applied loads
Highlight: Four targets already modified, including one “on deck”
Developing: Next generation design
Gas injection
Tapered wall
Full-penetration welds
[Winder, Target Breakout]

## Slide 15: Strain measurements in situ at SNS
Benefit: Direction for design
  Calibration of analysis
  Diagnostic for gas injection and other design changes
Highlight: Strain data already collected
Developing: More extensive data (time and space)
Strain sensors on target vessel
Beam Pulse Strain Measurement
[Wendel, Target Breakout]
Calculation
Measurement

## Slide 16: Fabrication improvements
Benefit: Reduce fabrication vulnerabilities
Highlight: TIG vs. E-beam welding mock-up
Developing: Weld distortion test, specifications update
Weld mockup for weld distortion test
New weld technique
[Winder, Target Breakout]

## Slide 17: Gas injection
Benefit: Reduction of pulsed structural loads and cavitation erosion
Highlight: Target retrofit fabrication begun
Developing: Gas supply, longer-term implementation
[Winder/Riemer, Target Breakout]

## Slide 18: Increased pump speed
Benefit: Lower thermal stresses and reduced beam-pulse induced cavitation
Highlight: Running successfully at 350 RPM
  Past 108 cycles at 1.4 MW
  Unexpected improvement of window flow
Developing: PIE of T13 and consideration of flow erosion experiments
Decreased
Window Flow
Inner wall cavitation damage
BEAM

## Slide 19: Improved PIE
Benefit: Truest source for design guidance
Highlight: T10 leak sample extracted with new tool
Developing: Characterization of specimens
Holes from cuts
Microscopy and metallurgical testing
[Baumgartner/Riemer, Target Breakout]

## Slide 20: These six current initiatives increase opportunity to reach reliability goal
Higher flow rate
  Already implemented on T13
Incremental changes to materials and geometry
  On-deck for installation (T14)
Modified jet-flow target to arrive in August, 2016
Early gas injection at low flow rate
  Should be ready in CY2017
Future design changes that directly address failure modes (e.g. recent results from T12)

## Slide 21: Target Breakout session
Overview of target station operations (M. Baumgartner)
Charge, and target strategies and resources (M. Wendel)
Information update
  PIE (B. Riemer)
  Instrumentation on target module (M. Wendel)
Design and Analysis (D. Winder)
Gas injection (B. Riemer)

## Slide 22: Summary
Much work was accomplished this year in response to 2015 DOE Review Committee recommendations
Short-term 1.4 MW goal is challenging, but may be within reach
Long-term 2+ MW goal will require more development effort
We need the committee advice on our priorities and strategies