## Slide 1: Challenges for Grazing Incidence Neutron Scattering at Pulsed Sources: Beyond basic experiments and data analysis
V. Lauter
Neutron Scattering Division
Oak Ridge National Laboratory, USA

## Slide 2: Collaborators & Acknowledgments
Scientific User Facilities Division, Office of Basic Energy Sciences, U.S. Department of Energy, Laboratory Directed Research&Development
Center for Nanophase Materials Science, ORNL
Rajeev Kumar,
Wei Li
Bobby Sumpter
University of Tennessee, Knoxville
J. P. Mahalik
Neutron Scattering Division, ORNL
Andrei Savici, Steven Hahn, Mathieu Doucet
Computational Sciences&Engineering
Division, ORNL
Eric Lingerfelt
Yawei Hui

## Slide 3: Outline
Grazing Incidence Neutron Scattering (GINS):
GINS= Specular reflection + off-specular scattering+ GISANS
Scattering in Time of Flight : advantages, difficulties & specifics
Structure
How can we obtain a precise correlation between the local interfacial characteristics and global physical properties?
Computational workflow
SCFT modeling as benchmark
Outlook
Development of workflow that can be extended and applied to other codes running on HPC

## Slide 4: Mesoscale control of thin film heterostructure materials - Why is it important?
Topological insulators
These novel materials are in need of characterizing their surfaces, boundary conditions and interfaces in the microscopic and mesoscopic length scales.
Spintronic devices
Multifunctional oxide
heterostructures
“Functionality often arises at the mesoscale, where defects, interfaces, and non-equilibrium structures are formed “,
From Quanta to the Continuum: Opportunities for Mesoscale Science, a report from the Basic Energy Sciences Advisory Committee (2012)
Structural characterization of multiple length scale with depth sensitivity
Bi-layer skyrmion
Liposome in electrolyte multilayers
Oriented graphene nanocomposites
Thermo-responsive multilayer films of ionic polymers&peptide

## Slide 5: Solving the problem: using effective tools for characterization
Structure and magnetization
Depth-sensitive with high resolution
Neutron Reflectometry – neutron grazing incidence method for thin films and heterostructures
Lauter et al. Nature 2016
Analysis of all three channels: specular reflection, off-specular scattering and GISANS allows to explore the systems quantitatively in three dimensions on enormous length scales
Qx
Qz
Qy
At present the majority of published data on reflectometry concerns only specular reflection
Rich information contained in off-specular data is not being exploited
Neutron Reflectometry: 3 scattering channels:
0.1-100mm length scale, Qx
1 - 100 nm length scale, Qy
Off-specular scattering
GISANS
Specular reflection
depth profile
lateral structure
lateral structure
0.5 nm resolution Qz
M. Wolf

## Slide 6
Field and current control of the electrical conductivity of an artificial two-dimensional honeycomb lattice
Deepak Singh et al, Missouri University, Columbia
Published March 2019
Artificial two-dimensional honeycomb lattice
Published February 2019
ITO Multilayer Thin Films for Patternable Transparent Electrodes
3D Nanoscale Mapping of Porosity in Solution-Processed ITO Multilayer Thin Films for Patternable Transparent Electrodes
Rosario Gerhardt et al, Georgia Tech, Atlanta
Voltage pulses synchronized with the pulsed neutron source were applied to a phospholipid bilayer membrane
Published July 2019
Voltage-Dependent Profile Structures of a Kv- Channel via Time-Resolved Neutron Interferometry
J. Kent Blasie et al, University of Pennsylvania
Recent publications from Magnetism Reflectometer at SNS

## Slide 7: Beyond basic experiment: Unique capability at Spallation Source: Grazing Incidence Neutron Scattering (GINS) for complete characterization and mesoscale control of thin film heterostructure materials
GINS experiments are being performed now at SNS
Advanced software tools for the analysis and modeling of Grazing Incidence Neutron Scattering (GINS) of complex heterostructures at the Spallation Neutron Source -> access to the interface driven properties
Despite the exceptional experimental capabilities, robust, dedicated and publicly available software for data analysis and modeling is not available to users
Theoretical formalism of the Distorted wave Born approximation (DWBA) for calculation of GINS is reported in the literature but is no relevant code exists
The rich information contained in these data is not being exploited without advanced software
GINS pilot experiment performed at the Magnetism Reflectometer at SNS on a multilayer heterostructure of magnetic Fe3O4 nanoparticles self-assembled in a block-copolymer matrix
V. Lauter et al, Reference Module Material Science and Materials
Engineering, Elsevier, 2016; ISBN: 978-0-12-803581-8
Time-of-flight
Off-specular scattering
GISANS
Specular reflection
depth profile
lateral structure
lateral structure
+
+
=
GINS
3D structure

## Slide 8: Novel approach towards exploration of mesoscale materials ?
Development of next generation data handling modus operandi for data analysis and modeling
Neutron Reflectometry Experiment
NSLD depth profile
Conventional reflectometry experiments provide only structural parameters via fitting model to the data
V. Lauter et al. , 2016
Can we obtain access to the interaction parameters causing this structure?
To realize this one needs a different approach to the data analysis

## Slide 9: Development of computational workflow capable of generating theoretical models in quantitative agreement with Grazing Incidence Neutron Scattering data (GINS)
The implementation of a computational workflow integrating high performance computing (HPC) with experiment via an intuitive, cross-platform user interface
TITAN
SCFT
simulations
cost-function
Minimizer
Experiment
Model
Theoretical
DWBA calculations
of GINS
User-friendly Interface
Computational Workflow
4
3
2
1
5
Beyond conventional data analysis

## Slide 10: Development of computational workflow capable of generating theoretical models in quantitative agreement with Grazing Incidence Neutron Scattering data (GINS)
The implementation of a computational workflow integrating high performance computing (HPC) with experiment via an intuitive, cross-platform user interface
TITAN
SCFT
simulations
cost-function
Minimizer
Experiment
Model
Theoretical
DWBA calculations
of GINS
User-friendly Interface
Computational Workflow
4
3
2
1
5
Phase diagram
A
B
f - volume fraction of component A
c - strength of interaction between A and B
Self-Consistent Field Theory (SCFT)
Beyond conventional data analysis

## Slide 11: Development of computational workflow capable of generating theoretical models in quantitative agreement with Grazing Incidence Neutron Scattering data (GINS)
The implementation of a computational workflow integrating high performance computing (HPC) with experiment via an intuitive, cross-platform user interface
TITAN
SCFT
simulations
cost-function
Minimizer
Experiment
Model
Theoretical
DWBA calculations
of GINS
User-friendly Interface
Computational Workflow
4
3
2
1
5
Phase diagram
A
B
f - volume fraction of component A
c - strength of interaction between A and B
Self-Consistent Field Theory (SCFT)
Beyond conventional data analysis

## Slide 12: Development of computational workflow capable of generating theoretical models in quantitative agreement with Grazing Incidence Neutron Scattering data (GINS)
The implementation of a computational workflow integrating high performance computing (HPC) with experiment via an intuitive, cross-platform user interface
TITAN
SCFT
simulations
cost-function
Minimizer
Experiment
Model
Theoretical
DWBA calculations
of GINS
User-friendly Interface
Computational Workflow
4
3
2
1
5
Phase diagram
A
B
f - volume fraction of component A
c - strength of interaction between A and B
Self-Consistent Field Theory (SCFT)
Beyond conventional data analysis

## Slide 13: Modeling Scheme: Self-Consistent Field Theory
Polymer-Polymer
Polymer-substrate
Polymer-air
dPS
PBMA
χS-BMA
χBMA-substrate
χS-Substrate
χS-Air
χBMA-Air
Polymer-nanoparticle
Fe2O3 core
PS corona
χS-NP
χBMA-NP
Hybrid SCFT scheme used for diblock copolymer nanocomposite thin films & Brownian dynamics of NPs
System: dPS-PBMA block copolymer thin film with or without hairy nanopartiles (Fe2O3 core and PS Corona), Lauter-Pasyuk et al, Langmuir, 19, 7783, 2003
Short range interaction parameter between different pairs fitted to match the scattering length density and neutron reflectivity profile of the experimental results.
melt of n A-B diblock copolymer chains confined between two parallel substrates
Local incompressibility constraint: sum of volume fractions of all the components (substrates, polymers, and nanoparticles) add up to 1
Numerical solution of the SCFT equations &Brownian dynamics of NPs
simulated using Polyswift++ (https://www.txcorp.com)

## Slide 14: 3D Volume fraction profile of different components in thin film obtained with SCFT
With 7% NP’s
Without NP’s
The nanoparticles preferentially accumulate at the center of the PS domains to avoid chain stretching penalty.
Parameters fixing length scales in the model:
Kuhn segment length (l),
average radius of the nanoparticle cores (Rp),
thickness of the nanoparticle corona (ξp),
polymer film thickness,
position (xa) and roughness of air interface (ξa), position (xs) and roughness (ξs) of the silica substrate

## Slide 15: Scattering Length Density
Lauter-Pasyuk et al, Langmuir, 19, 7783, 2003
Mahalik KP et al, Macromolecules, 2018
Laterally averaged volume fraction profiles of components:
Air interface,
SiO2 substrate,
dPS,
PnBMA,
NP

## Slide 16
Published on-line April 2018 [1]:
Macromolecules, 2018, 51 (8), pp 3116–3125

## Slide 17: Asymmetric block copolymer nanocomposite thin film – SCFT model for NR analysis
0%
5%
10%
substrate

## Slide 18
Development of hybrid particle-field based model for asymmetric co-polymer/nanoparticles systems
Silica Substrate
Air Interface
dPS-b-PBMA
dPS
PBMA
A=dPS
Fraction of A block, fA=NA/(NA+NB)=0.34
If l (Avg Kuhn length)=0.77 nm is used Rgo=13 nm
Film thickness D/Rgo ~ 4.2-4.4 Rgo
But l is a fitted parameter, must depend on the fA
𝛘N ~ 29-31 at 160 C
Species | Polymer MW (Da) | Monomer MW (Da) | N’ | 𝛒o-1 (g/mol) | N
dPS | 59400 | 112 | 530 | 114.5 | 578
PBMA | 107000 | 142 | 754 | 159 | 1142
Total | 166400 |  | 1284 | 140.6 | 1719
Ni’=Polymer_Mwi/Monomer_MWi
N’=𝚺Ni’
𝝆o-1N’=𝜮𝝆oi-1Ni’
Ni=𝝆R/𝝆oi
𝛒R-1=105 g/mol (corresponding to protonated PS)
R is the reference component

## Slide 19: Competing Structures in thin film
Air Interface
Silica Substrate
Structure 1: Cylinder
PBMA
dPS
Structure 2: Mixed
PBMA
dPS
𝞓F=Fmixed – Fcylinder > 0
Free energy difference between the mixed state and cylinder

## Slide 20: Effect of film thickness
Parameters
𝞆ABN=17
𝞆A-AirN=0.0
𝞆A-SiN=8
𝞆B-Air=-80
𝞆B-Si=0.0
Simulation box dimension in the horizontal direction was varied
to determine the free energy minima for different morphologies
With increase of film thickness ∆F decreases initially
Saturation of ∆F at certain thickness

## Slide 21: Effect of 𝞆N and thickness
Lower D/Rgo (5): Cylinder
PBMA
dPS
Higher D/Rgo (5.5) and higher 𝛘N: Lamellar
PBMA
dPS
𝛘N=17
𝛘N=30
Higher D/Rgo (5.5) and lower 𝛘N: Cylinder
PBMA
dPS
Lamellar
Cylinder
Matsen, Eur. Phys. J. E., 30 361, 2009
Thin Film results consistent with bulk results reported in literature
0.34

## Slide 22: Effect of polydispersity (polydisperse B block -PBMA)
PDI=1.0, NB=66
𝛘N=17 ; D/Rgo=5.0
PDI=1.2, <NB>=13.2
PDI=1.667, <NB>=44
𝛘N=25
15.4, 33.0, 56.4,86.0,122.7
167.4,221.7,288.1,371.8,485.4
10.1, 40.7, 92.4, 166.4, 264.9, 390.7
548.9, 747.6, 1002.8, 1355.5
10 quadratures
10 quadratures:
Parameters
𝞆ABN=17
𝞆A-AirN=0.0
𝞆A-SiN=0.0
𝞆B-Air=-80
𝞆B-Si=0.0
Higher polydispersity prefers the mixed domain at low 𝛘N but increasing 𝛘N leads to lamellar structure

## Slide 23: SLD comparison: Preliminary data
Modeled: Coexistence of cylinder and lamellar
Our SCFT based investigations revealed that a coexistence is thermodynamically stable in the presence of disperse majority block.
SCFT study clearly shows that vertical segregation based on chain lengths can lead to stabilization of cylinders near one substrate and lamellae near the other substrate.

## Slide 24: Development of a user-interface and computational workflow capable of generating SCFT models in quantitative agreement with GINS data
Architecture and Workflow
Our target is demonstration of running software suite for processing, modeling and fitting of GINS data
High Speed Data Transfer with Globus
LOCAL
From anywhere on www via XCAMS
(HTTPS)
SCFT Simulations/ HPC
GINS at SNS
UI
High Speed Data Transfer with Globus
Web & Data Server
CADES Storage
MySQL
Database
Data
& Artifacts
CADES Cluster Computing
SCFT Simulations
&
Theoretical
DWBA
Calculations
of GINS
Notes: The Compute and Data Environment for Science (CADES) at ORNL is providing a compute and data infrastructure coupled with experts in data science to create a new environment for scientific discovery.

## Slide 25: Developed User interface of GINS Simulator as part of the Data Analysis workflow
Interactive 2D colormap visualization
Animation movie controls
View currently selected values and modify data view dynamically
Save current data file as HDF5 and image as PNG
Select data view from tabbed interface

## Slide 26
We show that combination of GINS experiments with theoretical model in the computational workflow data provides a direct access to the physical properties.
The first results on the implementation of a computational workflow integrating high performance computing (HPC) with GINS experiment via an intuitive, cross-platform user interface being developed at SNS/ORNL
The simulation approach developed for block copolymers is general to predict microphase separation in thin films of any block copolymer nanocomposite with the specific details encoded in the interaction parameters.
Conclusions and outlook
Spallation neutron source delivers outstanding experimental conditions to perform simultaneously a combined measurement of specular reflection, OSS and GISANS using time-of-flight (TOF)

## Slide 27: Development of computational workflow capable of generating theoretical models in quantitative agreement with Grazing Incidence Neutron Scattering data (GINS)
The implementation of a computational workflow integrating high performance computing (HPC) with experiment via an intuitive, cross-platform user interface
TITAN
SCFT
simulations
cost-function
Minimizer
Experiment
Model
Theoretical
DWBA calculations
of GINS
User-friendly Interface
Computational Workflow
4
3
2
1
5
Beyond conventional data analysis
Self-Consistent Field Theory (SCFT)
(block copolymers)
Soft Matter
Density-functional theory (DFT)
Quantum Materials
Oxide heterostructures

## Slide 30
N_PS=34
10.1
40.7
92.4
166.4
264.9
390.7
548.9
747.6
1002.8
1355.5
N_BMA
Segregation of smaller PBMA chains near lamellar domain and larger PBMA chains near the substrate preferring curved structure