## Slide 1: Dissolve Next generation software for the analysis of total scattering data
Dr Tristan Youngs
Disordered Materials Group, ISIS Pulsed Neutron and Muon Source
STFC Rutherford Appleton Laboratory
Harwell Oxford, Didcot, Oxon, OX11 0QX

## Slide 2: Disordered Materials
Show predominantly local ordering (i.e. on the scale of atoms or molecules)
Show primarily diffuse scattering
Are typically dynamic (e.g. liquids) – average structural picture is obtained
May show long-range order (i.e. Bragg scattering)
May contain large length-scale correlations (e.g. micelles, lamellae)
Characteristic Properties
Liquids
Glasses
Solutions
Condensed phases
under confinement

## Slide 3: Disordered Materials Instrumentation
The Group’s Instruments
NIMROD
Near and InterMediate Range
Order Diffractometer
SANDALS
Small Angle Neutron Diffractometer
for Amorphous and Liquid Samples
GEM
General Materials Diffractometer

## Slide 5: The Total Structure Factor
All Disordered Materials instruments give access to the total structure factor
  Accessible Q range and target systems vary
Result of constructive interference between coherently scattered neutrons
  Promoted by correlations between atoms / molecules
Arises from:
  Chemical bonds within molecules
  Attractive forces between molecules
  Larger assemblies of molecules (e.g. micelles)
  Lattice planes etc.

## Slide 6: The Total Structure Factor
Water as an ice, a liquid, and a glass
Crystalline Solid
Liquid
Glass

## Slide 7: Linking Experiment and Theory
Instruments give total structure factor, and which is generally too complex and “fluffy” to interpret by inspection
Contains information on all of the structural correlations occurring within a given sample
  Only dependent on spatial arrangement of atoms
Classical simulation techniques have existed for many years, allowing real systems to be approximated on the atomic level by using empirical potential functions to describe the underlying interactions
  Simulates the spatial arrangement of atoms
BUT – instrument measures in Q-space, and simulations work in real-space…

## Slide 8: Linking Experiment and Theory
F(Q) and G(r) related by Fourier transform. Lucky!
Instrument
Real System
Total Structure Factor F(Q)
Computer
Simulated System
Total Radial Distribution Function G(r)
Reciprocal Space
Real Space
⇦ FT ⇨

## Slide 9: Basic Simulation
Published forcefield parameters describing many systems, so…
No
Yes
Agreement?
Compare
Tough!
Great, write the paper…
Forcefield

## Slide 10: Improving on a Basic Simulation
Need to have a forcefield-based simulation to interpret data in vast majority of cases – literature parameters exist for a variety of systems
How are these forcefield parameters obtained?
  Reproduction of thermodynamic properties
  Extrapolated / inferred from other systems
  Chosen to reproduce experimental structural data? NO!
Change these somehow to improve the agreement between simulation experiment?
  Tweaking by hand almost impossible
  Fitting algorithm could work, but parameter space is large

## Slide 11: Composition of the Total Structure Factor
Atom types and Partials
Total Structure Factor
(Experimental Observable)
Partial Structure Factor
(Accessed via Simulation)

## Slide 12: Partial Pair Correlations
An “atom type” is a specific kind of atom in the system
  Depends at least on the element. Can be split by chemical environment.
  Does not depend on isotope.
For example, water has two atom types – ‘O’ and ‘H’ – so there are three distinct partials: , , and
i
j
O
H
O
H
Argon
i
j
C
H2
C
H2
H1
O
Methanol
H1
O
i
j
C
H
C
H
O
O
Formaldehyde
i
j
O
H
O
H
Water
N = 1
Also N2, O2…
N = 3
Also benzene, silica…
N = 6
N = 10

## Slide 13: The Goal – Experimental S(Q)
Total structure factor is a useful quantity, but the real value is in the individual partial that constitute it
If we can obtain the partial then we have direct information on the pair correlation functions, and can manipulate this to infer pair potentials
But, can’t do this directly from a single measured dataset:
0.0374 | –0.0964 | 0.0622
=

## Slide 14: Isotopic Substitution
Change weightings of partials in the measured by changing isotope
  e.g. 2H for H, 15N for N, 6Li for Li
Key assumption: structure is independent of isotopes used
Perform multiple measurements on the same system, with different isotopic substitutions
The Power of Neutrons
x-ray |  |  |  |  | 
 |  |  | C | Al | Fe
n (bc) (fm) | –3.74 | 6.67 | 6.65 | 3.45 | 9.45
 | H | D (2H) |  |  | 
Scattering Lengths

## Slide 15: Inversion of the Scattering Matrix
Direct extraction of individual is possible for ‘simple’ systems
0.0374 | –0.0964 | 0.0622
0.0374 | 0.1722 | 0.1980
0.0374 | 0.0378 | –0.0277
=
4.8238 | –2.7037 | 24.6061
–5.8227 | 1.6265 | 4.1962
4.1525 | 4.1525 | –8.3050
=

## Slide 16: Potential Refinement
Take differences between experimental and simulated to get
Fit the using a suitable approximation (Poisson expansion)
Enter these into the inverse scattering matrix to generate
Fourier transform the into and use these to form an additional, empirical potential for each atom type pair
Repeatedly run the simulation and generate additional potentials until the experimental and simulated ‘match’
Generating an improved interaction potential
4.8238 | –2.7037 | 24.6061
–5.8227 | 1.6265 | 4.1962
4.1525 | 4.1525 | –8.3050
=

## Slide 17: “Enhanced” Simulation
FT–1
Take
Difference
Experimental datasets actively used to derive new pair potentials
No
Yes
Agreement?
Compare
Great, write the paper…
FT

## Slide 18: Liquid Water
Structure Factors / Total G(r)

## Slide 19: Liquid Water
Optimised Forcefield / Augmented Potentials
Parameter | SPC-Fw | Optimised
q(O) | –0.82 e | (empirical)
q(H) | 0.41 e | (empirical)
σ(O) | 3.165 Å | (empirical)
ε(O) | 0.6503 kJ mol–1 | (empirical)
σ(H) | -- | (empirical)
ε(H) | -- | (empirical)
r(O–H) | 1.0 Å | 0.975 Å
k(O–H) | 4431.53 kJ mol–1 Å–2 | 
θ(H–O–H) | 113.24° | 104.0°
k(H–O–H) | 317.57 kJ mol–1 rad–2 | 

## Slide 20: Isotope Availability & Access
For many systems, there are too few isotopic sample possibilities available
  Elements for which there are no suitable isotope pairs
  Isotopic exchange prohibited by difficulty in synthesising target compounds
  System complexity means there may be too many measurements to make in the timescale of a reasonable experiment
For instance, silica:
No inversion possible, so no access to partial
0.0191 | 0.1070 | 0.1497
=

## Slide 21: Generalisation
What is a general method to allow inversion of the underdetermined case?
Use the simulation? It has all the partials we need, which are hopefully a good “guess” for the experimental ones
Define a feedback factor, , and write new weights factors…
The Augmented Scattering Matrix
0.0191 | 0.1070 | 0.1497
=

## Slide 22: The Augmented Scattering Matrix
For each partial in the simulation, add a row to the scattering matrix weighted by
Typically,
Now have an overdetermined matrix for which we can find a (pseudo) inverse
Generalised Access to S(Q)
0.0172 | 0.0963 | 0.1347
0.1 | 0.0 | 0.0
0.0 | 0.1 | 0.0
0.0 | 0.0 | 0.1
=

## Slide 23: Empirical Potential Structure Refinement
Developed and maintained by Prof. Alan Soper
Creation driven by scientific interest, and which went on to fulfil the needs of other users who became the Disordered Materials community
Proven on a variety of systems – pure liquids, liquid mixtures, polymers, confined liquids in porous media etc.
80% of SANDALS publications use EPSR
Chem. Phys. 202, 295 (1996); Mol. Phys. 99, 1503 (2001);
Phys Rev. B 72, 104204 (2005)
The Disordered Materials Workhorse

## Slide 24: Five Caveats with EPSR
Limited to ~ 140 k atoms in a simulation
  At water liquid density ⇒ ~110 Å box length ⇒ 55 Å correlation length max
Single configuration / single simulation
  One atomic configuration at a time, subject to the same algorithms
Custom forcefield – not so good at handling large / floppy molecules
  Not a “standard” classical forcefield
Parallel via OpenMP – limited to running on a single enclosure
Author retired!

## Slide 25: Evolving Science
Not Getting Any Easier…
Component
Size
System
Complexity
System
Size
Pure Liquids
Mixtures / Solutes
Confined Liquids / Mixtures
Reacting Mixtures / Amorphous Solids / Disordered Crystals
Single Phase
Small / “Simple”
Moderate
Large / Flexible
Multiple Phase
Dynamic / Ill-defined Phase
Crystals
Biological

## Slide 26: Current / Future Applications
Solvated macromolecules
Dilute systems, mostly solvent
  Solvent-solute structuring often primary concern
  Interaction between solutes is also of interest
  Flexibility and conformation of molecules
⇒ Requires million atom simulations
⇒ Require proper intramolecular description of the protein
⇒ Molecular dynamics required to usefully relax the protein (in addition to Monte Carlo)

## Slide 27: Current / New Applications
Pore filling of porous silicates
Liquids confined in imperfect lattices
  Variance of substrate
    Pore size, surface roughness, surface hydroxylation
  Variance of deposited liquid
    Degree of pore filling
    Composition fo pore filling in mixed systems
⇒ Procedural, parameterised generation of configurations
⇒ Multiple configurations required to account for structural diversity

## Slide 28: Current / New Applications
Interfaces
Laponite suspensions
  Periodic “platelet” in original study
  Simulate free platelet(s) in solution
⇒ Large system sizes
⇒ Specific forcefield terms for platelets required
Nanotubes
  Low concentrations of solute / surface
  Account for polydispersity (realism)
⇒ Multiple configurations / procedural generation
⇒ Need for “exotic” analysis of the structure

## Slide 29: Current / New Applications
Macromolecular aggregates
Asphaltenes in solution
  Aggregation of large molecules with variable size and structure
Micelle formation
  Account for multiple micelle formation
⇒ Million atom simulations
Variable or ill-defined bonding
Metal organic framework melts
  Ability to study melting – need to “sit” between crystal and liquid
Proton-transfer in acid-base systems
⇒ Explore macroscopic parameters as part of refinement

## Slide 30: Dissolve
Find Dissolve on GitHub (trisyoungs/dissolve)
Preliminary paper at: https://doi.org/10.1080/00268976.2019.1651918
Current State:
Full classical forcefield engine
Monte Carlo and molecular dynamics evolution
Million atom capable / parallelised with OpenMPI
Fully customisable simulation – “do what the system needs”
Basic procedural generation of configurations
Analysis framework – built-in quantity calculation / also user-definable
Full GUI for setting up / monitoring / analysing simulations