## Slide 1: Scope and Status of Materials Research for Source Technologies at ESS
Yong Joong Lee
ICANS XXIII, Chattanooga
October 14, 2019

## Slide 2: ESS Target Environment
Proton beam (2 GeV/5 MW)
Proton Beam Instrumentation
Proton Beam Window (PBW)
Moderator Reflector
Target Wheel
Target Wheel Drive Unit
Beam Extraction Unit

## Slide 3: Materials Research in Target Environment
Degradation of functional and structural materials in target environment poses challenges to operational reliability and costs.
The materials research at ESS is dedicated to
  Selection of materials which endures intense radiation field in target environment
  Determination of component lifetime, which are subject to radiation damage
  Realization of the visions of materials R&D at ESS
  Contributions to the high power target community with the knowledge acquired
Motivation and Mission

## Slide 4: Status Overview of Materials Activities
Spallation Materials
Mechanical Properties
Oxidation Properties
Proton Beam Window Materials
BLIP Irradiation Campaign
PIE of STIP Specimens: Al6061-T6, Alloy 718, Ti-6Al-4V
PIE of STIP-V Specimens
RI Beam Irrad. Campaign & PIE
Moderator Materials
Measurement Tech for Ortho-Para H2
Conversion Kinetics of Ortho-Para H2
Beryllium XS Characterization
Beam-Material Interaction
Dynamic Response of W to Raster
Beam Intercepting Diagnostic Devices
LINAC Beam Dump
Beam Conditions on Target
Polymeric Materials
Irradi. Campaign & PIE of Elastomers
Irrad. Campaign & PIE of Grease
Materials Lab
SEM
Optical Microscope
EDX
Project Support
Materials Handbook
Materials Selection & Lifetime Criteria
Multiphysics Analyses
Tritium Release, Water Radiolysis, Corrosion Issues
Future Projects
Irradiation Module
Proposals for External Grants
Muography for TG Monitoring
Elemental Analyses
Structural Behavior of Coated Al6061
LFA
Water-cooled Back-up Target
Colour | Status Description
 | Completed
 | Ongoing
 | Failed and Activity Closed
 | In Plan (External Funding)

## Slide 5: Project Support
Define selection criteria and lifetimes of materials that are subject to hadron and gamma radiation doses.
Record decisions regarding materials, which are made in consensus between the Materials Group and the relevant sub-project unit, and the reasoning behind such decisions.
Compile material properties data to serve for the engineering of the ESS systems in target and accelerator environments.
ESS Materials Handbook
Period |  | Main Activities and Milestones
Start | Finish | 
Jan 1, 2015 | Dec 31, 2019 | Real-time compilation of project materials data in place
Dec 31, 2019 |  | Completion of CDR of all sub-projects and design freeze
Jan 1, 2020 | Dec 31, 2020 | Compilation of all required project materials data in place
Jun 30, 2021 |  | Preliminary version release and start of review process
Jun 30, 2021 | Dec 31, 2021 | Final editing and review of each completed section
Dec 31, 2021 |  | Release of the final version

## Slide 6: Materials Lab (Hossein Sina)
Provide Services for Materials Characterisation
Currently Equipped with SEM/EDS, LFA and Optical Microscope

## Slide 7: Spallation Materials: Tungsten (J. Habainy)
Tensile and Fatigue Tests (Lund U)
  Define the operational stress range
  Define the quality criteria in choosing tungsten grade
  Vendor evaluation
Oxidation Tests (Lund U)
  Define the operational temperature range
  Provide inputs for hazard analysis
PIE of STIP-V specimens (PSI)
  Proton induced degradation of mechanical properties
  Proton induced degradation of thermal properties
  Proton induced change in microstructure
PIE of RI beam irradiated W (GSI, PSI, Darlana U)
  Displacement damage induced degradation of mechanical and thermal properties
  Dynamic response of oxide layer to the pulsed beam
Release fraction (DTU)
Erosion and oxide aerosol release (Lund U)
Work Scope

## Slide 8: Spallation Materials: Tungsten
Project status: Competed except
  LFA and mechanical tests of high dose STIP-V samples
Design requirements:
  The surface temperature of tungsten shall be lower than 500 C during normal operation.
  The surface temperature of tungsten shall be lower than 700 C in loss of coolant accidents.
  The steady state equivalent stress in tungsten shall be lower than 100 MPa.
  The beam pulse induced stress amplitude in tungsten shall be lower than 50 MPa.
Radiation Impacts:
  Reduced strength and ductility
  Reduced thermal conductivity
  Potential stiffening
Post pulse
-20% therm. cond.
+ 20% stiffness
+ 25 MPa
Equivalent stress

## Slide 9: Proton Beam Window Materials
PBW is exposed to the highest flux of protons
  Short lifetime
  Challenge in operation and maintenance
BLIP Irradiation Program (RaDIATE Collaboration)
  Al5754-O
  Al6061-T6
STIP Program (PSI)
  Materials:
    Al6061-T6 (STIP-VII)
    Alloy 718 (STIP-II)
    Ti-6Al-4V (STIP-VII)
  Status: Project Launched
    PIE of alloy 718 planned in 2019

## Slide 10: Moderator Materials
Challenges:
  The brightness of the ESS neutron beam is dependent on a high para fraction of liquid hydrogen
  Neutrons and gamma back convert para-H2 into the ortho state
  Required to keep converting ortho-H2 back to para
Investigated Areas:
  In situ Raman spectroscopy technologies
  In situ vibrational spectroscopy technologies (SNS)
  Conversion kinetics of catalysers
  In beam measurement of ortho-para fraction (J-PARC)
  Safety measure and licensing of sapphire window
Liquid Hydrogen
Emil Karlsson, MSc Thesis, Lund U
More details:
Monika Hartl, 12:10 PM, Oct 15
Moderators and Reflectors Session

## Slide 11: Moderators and Reflectors
Beryllium Selection Criteria
  Isotropic texture
  Small grain size
  High purity
Research on the correlation between neutron scattering cross-section and different beryllium grades is launched
  S-65: Vacuum Hot Pressed
  S-65-H: Hot Isostatic Pressed
  S-200-F: Vacuum Hot Pressed
  Sintered/Forged Be from Ulba
Investigated areas:
  Grain structure and elemental characteristics (Slava Kuksenko, UKAEA)
  Neutron scattering experiments (LANSCE)
Beryllium
More details:
Douglas Di Julio, 10:30 AM, Oct 15
Moderators and Reflectors Session

## Slide 12: Polymeric Materials: LENA Irradiation Campaign
TRIGA MARK-II Nuclear Research Reactor in Pavia
  250 kW maximum power
  Central thimble with a diameter of 3.8 cm houses the test specimens
  Total maximum neutron flux: 1.72e13 neutron/cm2/s
    Thermal (E < 0.8 eV): 6.75e12 neutron/cm2/s
    Fast (E > 0.5 MeV): 3.80e12 neutron/cm2/s
  Maximum irradiation temperature: 60 C
Matteo Ferrari

## Slide 13: Polymeric Materials : PIE of Elastomers
Matteo Ferrari

## Slide 14: Polymeric Materials : PIE of Lubricants
Project Status: Completed
  Grease types in neutron heavy environment is recommended
  Elastomer types in neutron heavy environment is recommended
Significant difference in damage rates between the gamma irradiated and neutron irradiated grease base oil has been identified.
Matteo Ferrari

## Slide 15: Raster Beam and Tungsten Interaction
H. D. Thomsen

## Slide 16: Raster Beam and Tungsten Interaction
Risk of coherency between the raster frequency and resonance mode of tungsten brick is identified.
Mechanical resonance test are performed for different temperatures and data analysis is in progress.
Decisions on MPS parameters for beam on target condition are in progress.
Prospect for 2019
Measurement performed by Henk Nolles, UKAEA

## Slide 17: Future Project
Irradiation Module

## Slide 18: Future Projects
Parasitic production of medical isotopes
  Conceptual Design Study
  Operational Model Study
  Identification and Teaming-Up of Potential Stakeholders
Muon radiography of target internal structure
  Cosmic-ray muons for 3D imaging of target internal structure in beam-off condition
  Spallation muons for 2D imaging of target internal structure in beam-on condition
Feasibility Studies for Exploring Opportunities for Research Grant
G. Yang et al. / Philosophical Transactions of the
Royal Society A, 377(2137), Dec 2018

## Slide 19: Summary
ESS Project is actively progressing with focus on installation, integration and commissioning
While actively serving for various subproject work packages, materials research at ESS begins to prepare its role for initial operation
Currently, main focus is to manage Materials Handbook towards its release planned in end 2021

## Slide 20
Thank You for Your Attention!