## Slide 1: Achievements in In-Situ Plasma Processing of High-beta Cavities
SNS AAC
February 16-18, 2016
Marc Doleans
SCL systems group

## Slide 2: In-situ plasma processing to increase linac energy
Higher linac energy provides more margin for reliable operation at 1.4 MW
Most cavities at SNS are limited by field emission (FE) leading to thermal instability in end-groups
  Average accelerating gradients are 12 and 13 MV/m for the two cavity geometries
Developed in-situ plasma processing to reduce FE and increase accelerating gradients
In-situ plasma processing

## Slide 3: First plasma processing of a cryomodule in the SNS linac tunnel is a success !
Plasma processed cryomodule slot 19 (CM00023)
Average accelerating gradient
  11.2 MV/m before plasma processing
  14.2 MV/m after plasma processing
Beam energy increase from plasma processing of slot 19
  ~11 MeV
+2.3 MV/m
+5.5 MV/m
+3.7 MV/m
+0.3 MV/m
Operating gradients increased !

## Slide 4: Since last review
Plasma processed and tested one more cavity in HTA (HB52)
Plasma processed offline cryomodule in RFTF test cave (CM00012)
Plasma processed cryomodule in-situ in the linac tunnel (CM00023)

## Slide 5: Deployment in linac tunnel started!
R&D with Nb samples and offline cavities
In-situ processing in linac tunnel
Processing of cryomodule in test cave
1st phase
2nd phase
4th phase
3rd phase
Processing of 6-cell cavity in HTA*
On-going
FY16
FY17
*HTA: Horizontal Test Apparatus
HB52
CM00012
CM00023

## Slide 6: PLASMA PROCESSING 2nd cavity in HTA (HB52)

## Slide 7: Plasma processing reduces Field emission and Secondary Emission Yield
SNS HB cavities show multipacting activity between 9 and 14 MV/m
  Normally reduces after RF conditioning and cavity performance then limited by FE
  Some cavities have severe multipacting which limits their performance
Cavity HB52 performance initially limited by multipacting
  Severity of end-group heating significantly reduced after plasma processing
Temp. increase of end-groups cooling circuit

## Slide 8: PLASMA PROCESSING OFFLINE CRYOMODULE (CM00012)

## Slide 9: 1st Plasma processing of a cryomodule
Offline cryomodule in RFTF test Cave (CM00012)
Plasma processing hardware for cryomodule
  Plasma process gas cart (new)
  Plasma RF cart
Plasma processing recipe successful for 4 cavities of HB cryomodule
1st plasma in a cryomodule !
New plasma processing cart for cryomodules

## Slide 10: Hydrocarbons in CM00012 cryomodule
Estimated amount of hydrocarbons removed
  Done by Integration of RGA signal from oxidation by-products such as CO2
  Few monolayers equivalent
Multiple cleaning cycles done over 2-3 weeks
  Used lessons learned from plasma processing of cavities in HTA
    Possible resurgence of hydrocarbons at top surface after cleaning over time
    Best cleaning obtained using multiple cycles

## Slide 11: Plasma processing of CM00012 cryomodule
Removal of hydrocarbons from all 4 cavities (A, B, C, D)
  Systematic estimation of removed amount
Several monolayers equivalent removed from each cavity
  ~2/3 of cells cleaned adequately
  ~1/3 cells could benefit from additional plasma cleaning

## Slide 12: Total hydrocarbon removed from CM00012
End cells of cavities are found to be most contaminated
Worse cells are at extremities of cryomodule
Beneficial to spend more time plasma processing cells with largest contamination
  Lesson learned applied during cleaning of CM00023 in tunnel

## Slide 13: Radiation level reduced after plasma processing
Cav A and D radiation dominated by field emission
Cav B and C radiation dominated by multipacting
Plasma processing reduced radiation level at given gradient in all cavities

## Slide 14: Performance of CM00012 cryomodule improved after plasma processing
Stable accelerating gradient at 60 Hz improved for all 4 cavities
Gradients improved by ~25%
  Avg. gradient 12.3 MV/m before plasma processing
  Avg. gradient 15.3 MV/m after plasma processing
  Cavity A improved by 35%
  Cavity B improved by 15%
    Initially limited by combination of multipacting and hot spot in end group
    Plasma processing reduced severity of multipacting which helped improving performance
      Reached >18 MV/m at low rep. rate with low radiation signal
    Hotspot limits performance at 60 Hz
Ready to deploy plasma processing in linac tunnel

## Slide 15: PLASMA PROCESSING CRYOMODULE SLOT 19 (CM00023)

## Slide 16: Vacuum connections for plasma processing
Warm up three cryomodules
  Slot 18, 19 and 20
Beamline turbo carts (turbo) on each cryomodule and warm sections
Plasma gas manifold cart to inject gas cavity D side
  Connections at cryomodules using standard cleanroom and 3nm pore size particulate filter
  Non-flammable gas cylinders and 16psig relief valve (< cryomodule relief pressure)
Pumping /monitoring of process gases
  Pirani gauges at connections inlet and outlet of cryomodule and RGA analysis
Slot 20
Slot 19
Slot 18
WS 19
WS 18
BL
C1
PLS
C2
RGA
D2
BL
D1
BL
E1
BL
B1
BL
A1
WS 17
A
Beam direction
B
C
D
E
SGV
18501
SGV
19001
SGV
19501
SGV
20001
SGV
17501
SGV
18001
SGV
20501
BL: Beamline turbo cart
CCG: Cold Cathode Gauge
IP: Ion Pump
PLS: Plasma gas manifold cart
RGA: Turbo cart with RGA
SGV: Sector Gate Valve
A, B, C, D & E: Angle valves

## Slide 17
WS 19
CM slot 19
Pumping port on CM
with angle valve
(serial number CM00023)
Downstream
C

## Slide 18
Pumping port on WS
with angle valve
WS 18
CM slot 18
Downstream
D

## Slide 19: Plasma processing hardware adjacent to CM slot 19
Applied ALARA: Radiation survey indicated best location for minimum radiation exposure during work (<1 mrem/hr)

## Slide 20: Vacuum configuration during plasma processing
Sections seeing process gas during processing: CM slot 19 and WS 18
  Ion pumps and CCGs off
Adjacent sections not seeing process gas
  3 gate valves closed on each side to protect nearest cold cryomodules (slots 17 & 21)
    Local mode only to avoid any accidental opening
  IP on and extra pumping using beamline turbo carts (WS19 and CM slots 18 and 20)
Slot 20
Slot 19
Slot 18
WS 19
WS 18
WS 17
10-8 Torr
10-6 Torr
10-1 Torr
10-6 Torr
10-1 Torr
10-8 Torr
Closed - Local mode
Closed - Local mode
warm
warm
warm
IPon
IPon
IPoff
IPoff
IPon
IPon
Opened - Local mode
A
B
C
D
E
BL
C1
PLS
C2
RGA
D2
BL
D1
BL
E1
BL
B1
BL
A1
SGV
19001
BL: Beamline turbo cart
CCG: Cold Cathode Gauge
IP: Ion Pump
PLS: Plasma gas manifold cart
RGA: Turbo cart with RGA
SGV: Sector Gate Valve
A, B, C, D & E: Angle valves

## Slide 21: RF configuration during plasma processing
C
All cavities disconnected from High power RF system
High power top-hats on each cavity
  Air side of coupler assemblies stay on at all time
Cavities processed sequentially and iteratively
  Following gas flow from cavity D to A
Cavity being plasma processed
  FPC and field probe connected to RF cart
  Camera monitors any discharge in FPC
A
B
gas
flow
D
FP
Plasma
RF
Cart
top view
FPC

## Slide 22: Radiation monitors for evaluating performance before/after plasma processing
D
C
Radiation waveforms during cavity operation at cold
  Helpful for rf conditioning
  Relevant diagnostic to quantify and understand cavity performance
PMTs have better sensitivity for detection of X-rays from cavity operation
  4 PMTs temporarily installed in the tunnel at slot 19
  Used to evaluate radiation level for each cavity before and after plasma processing
B
A
PMT4
PMT3
PMT2
PMT1
side view
“Dev03”
“DBLM21”
“DBLM24”
“DBLM18”

## Slide 23: Plasma processing of CM00023 cryomodule
Removal of hydrocarbons from all 4 cavities (A, B, C, D)
  Blind tunning, RF probe signal useful to confirm location of plasma
Several monolayers equivalent removed from each cavity
  Contamination pattern similar to offline cryomodule
  Used lesson learned and plasma processed cavity extremities more

## Slide 24: First in-situ plasma cleaning of hydrocarbons in linac tunnel achieved!
Similar contamination pattern as offline cryomodule
Multiple RF carts would allow to plasma process cavities simultaneously
  Reduce amount of time needed for plasma processing
    Further improve on ALARA (less time in the tunnel)
    Facilitate coordination with other work in tunnel during maintenance period

## Slide 25: Radiation level reduced after plasma processing
Plasma processing reduced radiation level at given gradient in all cavities
Cavities more stable even at higher radiation level after plasma processing

## Slide 26: Performance of CM00023 cryomodule improved after plasma processing
Stable accelerating gradient at 60 Hz improved for all 4 cavities
Gradients improved by ~25%
  Avg. gradient 11.2 MV/m before plasma processing
  Avg. gradient 14.2 MV/m after plasma processing
  Cavity B improved by 60%
  Cavity D barely improved
    Strong emitter affects all cavities
    Ion pump burst at restart
      Affected cavity D?
      Dedicated study with offline cavity will be conducted

## Slide 27: CONCLUSION
Plasma processing effort is going very well
Plasma processing of offline cryomodule was a success
  Total accelerating gradient increased by ~12 MV/m
  Not yet re-installed in linac tunnel
First plasma processing of a cryomodule in SNS tunnel is a success!
  Total accelerating gradient increased by ~12 MV/m
  Corresponding beam energy increase ~11 MeV
Main deployment of plasma processing in SNS linac tunnel for high-beta cryomodules foreseen for FY16 and FY17
Plasma processing of medium-beta cryomodules is anticipated during Proton Power Upgrade
  Efficient use of existing RF power in SC linac

## Slide 28: Multipacting and FE radiation
Radiation monitors useful diagnostics to assess cavity performance
  Waveform during RF pulse informs about type of electron activity
  Integrated value per pulse simple value of merit for electron activity
  Radiation associated to multipacting tend to saturate after multipacting band is passed
  Radiation associated to FE follow the electric field waveform and keep increasing