## Slide 1: Muon Spin Rotation/Relaxation as a Probe of Unconventional Superconductivity
Graeme Luke
McMaster University

## Slide 2: Superconductivity
𝛒=0, M=-1.0 (SI)
Thermodynamic phase transition (Cp)
2Δ= Energy to split Cooper pair
  Order parameter for S.C.
Measure directly
  Tunneling, ARPES
Indirectly via quasiparticles
  specific heat
  penetration depth

## Slide 3: Unconventional Superconductivity
Conventional
Δ(k) has symmetry of crystal
Usually Δ(k)=Δ (s-wave)
Δ
Δ=Δ
Unconventional
Δ(k) has lower symmetry
Possible nodes in gap.
Other broken symmetries

## Slide 4: Sr2RuO4
Maeno et al., Nature 372, 532 (1994).
1st superconducting layered perovskite w/o Cu.
Isostructural to La2CuO4
Stoichiometric Sr2RuO4: metallic and superconducting

## Slide 5: Sr2RuO4 Normal State
Anisotropic 3-D metal
T<25K: 𝛒~T2 (Fermi liquid)
𝛒c/𝛒ab~1400
Mackenzie et al., Phys. Rev. Lett. 76, 3786 (1996).
Hussey et al., Phys. Rev. B 57, 5505 (1998).
Bergemann et al., Adv. Phys. 52, 639 (2003).
Damascelli et al., Phys. Rev. Lett. 85, 5196 (2000).
α
β
γ

## Slide 6: Superconducting State
Dependence of Tc on 𝛒0
Extreme sensitivity to (non)-magnetic impurities
Mackenzie et al., Phys. Rev. Lett. 80, 161 (1998).

## Slide 7: Anisotropic Pairing? - NMR
power law 1/T1, no Hebel-Slichter peak.
spin susceptibility unchanged below Tc.
Ishida et al., Phys. Rev. B 56, R505 (1997).
Ishida et al., Phys. Rev. Lett. 84, 5387 (2000).
Ishida et al., Nature 396, 658 (1998).

## Slide 8: Anisotropic Pairing?
Induced moment form factor (Neutron)
  No change of spin susceptibility below Tc.
  consistent with spin triplet: kx±iky state.
Duffy et al., Phys. Rev. Lett. 85, 5412 (2000).

## Slide 9: Muon Spin Rotation
  π+ → µ+ + υµ. (26ns)
    100% muon polarization
  µ+ →e+ + 2 neutrinos
    ~1/3 polarization.

## Slide 10: Experimental Geometry
τμ=2.2μs

## Slide 11: Capabilities at TCMMS
HiTime: 7.5T, 1GHz, 2K
Low Background
DR: 20mK, 5T
High Pressure:
22kbar, 2.5K, 55% sample

## Slide 12
Zero Field ZF-μSR
Ordered state, ν∝ Moment ∝√IB
Random frozen spins give characteristic relaxation.
Carlo et al., Nat. Mat. 11, 323 (2012).

## Slide 13: Broken Time Reversal Symmetry
Surfaces, domain walls, defects generate physical supercurrents and magnetic fields.
  eg. kx+iky/kx-iky
j(x)
B(x)
Sigrist & Ueda, R.M.P. 63, 239 (1991).

## Slide 14: Sr2RuO4: ZF-μSR
Luke et al., Nature 394, 156 (1998).
Luke and Sonier, Physics in Canada 67, 93 (2011).

## Slide 15: Polar Kerr Effect
Kerr rotation in trained samples below Tc.
Xia et al., Phys. Rev. Lett. 97, 167002 (2006).

## Slide 16: Surface Probes
No supercurrents detected at surfaces of Sr2RuO4.
Hicks et al., Phys. Rev. B 81, 214501 (2010).
Kirtley et al., Phys. Rev. B 76, 014526 (2007).
Tunneling detects edge states
Kashiwaya et al., Phys. Rev. Lett. 107, 077003 (2011).

## Slide 17: PrOs4Sb12
ZF-μSR
Aoki et al., Phys. Rev. Lett. 91, 1067003 (2003).
Scanning SQUID - no evidence for surface currents.
Hicks et al., Phys. Rev. B 81, 214501 (2010).

## Slide 18: UPt3
ZF-μSR
  spontaneous local field below Tc-.
  Not seen in Europe.
Kerr rotation
  below Tc-.
Luke et al., Phys. Rev. Lett. 71, 1466 (1993).
Schemm et al., Science 345, 190 (2014).
Dalmas de Reotier et al., Phys. Lett. A 205, 239 (1995).

## Slide 19: Non-Centrosymmetric Superconductors
SrPtAs
LaPt3Si
Biswas et al., Phys. Rev. B 87, 180503R (2013).
Kawasaki et al., JPSJ 82, 084713 (2013).

## Slide 20: Topological Superconductors
CuxBi2Se3
Sn1-xInxTe
Sasaki et al., PRL 107, 217001 (2011).

## Slide 21: Sr2RuO4 Electrodynamics
ZF-μSR gives broken time reversal symmetry.
kx±iky most likely state.
  state is nodeless (gap magnitude constant).
Evidence for gap nodes
  Power laws in specific heat, ultrasound attenuation, thermal conductivity…
Nishizaki et al., JPSJ 69, 572 (2000).
Lupien et al., PRL 86, 5986 (2001).

## Slide 22: Vortex State
2 lengthscales: λ, ξ
Disorder: broadening of line shape features (convolute with Gaussian).
Ceramics - Gaussian
Sonier, Rep. Prog. Phys. 70, 1717 (2007).
J.C. Davis website

## Slide 23: Vortex Lattice Field Distribution
Yaouanc et al., Phys. Rev. B 55, 11107 (1997).
V3Si

## Slide 24: Ba(Fe1-xCox)2As2 Superfluid Properties
Text
Williams et al., PRB 82, 094512 (2010).
s±➞d gap
with Co doping ↑

## Slide 25: Sr2RuO4: Square Vortex Lattice - SANS
Riseman et al., Nature 396, 242 (1998).

## Slide 26: Vortex Lattice - Agterberg
G.L. Theory for a 2-component order parameter with B//c.
Detailed comparison with small angle neutron scattering favours Agterberg model.
1Comp. G.L.
Agterberg ν=.2
Observed
Kealey et al., Phys. Rev. Lett. 84, 6094 (2000).

## Slide 27: Sr2RuO4 Vortex Lattice Geometry
broadened for 𝞃μ, disorder.
B.G.

## Slide 28: Sr2RuO4 TF-μSR Analysis
Square lattice data fit to microscopic Agterberg theory.
Triangular lattice fit to Ginzburg-Landau model.
Obtain κ for each field from global fit, then extract λ(T,H).

## Slide 29: Superfluid Density
Fit to weak coupled BCS.
Neutrons give 194nm at 20mT
all bands give 100nm
γ alone gives 171nm.

## Slide 30: c-axis
λc(0)=4000nm.
No evidence for nodes.
1/λ2=1/λcλab

## Slide 31: (Ir,Pt)Te2
Layered structure
High spin orbit coupling
Structural transition
Ir Te
Feng et al., Sci. Rep. 3 1153 2013
Yang et al., PRL 108 116402 (2012)
Matsumoto et al., JLTP 1999

## Slide 32: (Ir,Pt)Te2 Superconducting Tc

## Slide 33: (Ir,Pt)Te2 TF-µSR

## Slide 34: (Ir,Pt)Te2 Reversible Magnetization
Wilson et al., 1605.04296

## Slide 35: (Ir,Pt)Te2 Penetration Depth
Wilson et al., 1605.04296
Fits to ns(T) give

## Slide 36: Conclusions
Broken time reversal in an expanding list of superconductors.
Sr2RuO4 likely chiral p-wave state (topological).
No obvious pattern for broken time-reversal, gap nodes.
µSR highly sensitive to magnetic field penetration depth in the intermediate state.

## Slide 37: Collaborators (Partial)
McMaster: M. Wilson, T. Munsie, A. Hallas, Y. Cai
Columbia: Y.J. Uemura, T. Goko
SFU: S.A. Sabok-Sayr, J.E. Sonier
Kyoto: Y. Maeno, Z.Q. Mao, Y. Mori
Wisconsin: D.F. Agterberg
ORNL,Knoxville: J. Yan, D. Mandrus