## Slide 1
Energy scales of unconventional superconductors
measured by muons and neutrons
Yasutomo J. Uemura, Columbia University, USA
ORNL New Science and Applications at SNS Workshop
2026 June 10-12

## Slide 2
TF 2kG
exp(-s2t2/2)
relaxation rate s
~ 1000 A for 1 kG

## Slide 3
l(T=0) = 4800 A
Relaxation rate

## Slide 4
UBC x-tal
Uemura et al. PRL 1989

## Slide 5
~ ns /m*

## Slide 6
BEC BCS Crossover
Phase Coherence

## Slide 7
BE-BCS
crossover
Uemura
1994
Retardation: charge energy (kTF) vs. mediator energy (hwB)
Fermions (e)
Fermions (e) + Bosons (2e)

## Slide 8
Why is Tc reduced from TBEC ?
4He: TBEC = 3.2 K
TC = 2.2 K
Cuprates:
TBEC / TC ~ 5

## Slide 9
Neutron magnetic resonance mode
Analogy with rotons in superfluid 4He
Role of competing order

## Slide 10
Rotons in bulk He
TBE = 3.2 K Tl = 2.2 K due to rotons
Rotons: Soft phonons for solidification of He --- competing state
solid He (66 atm)
1962

## Slide 11
Tc of the bosonic superfluid 3-d 4He
determined by the soft mode energy
towards competing state.
2
1
0
0.0
1.0

## Slide 13
2
1
0
0.0
1.0
spin gap energy

## Slide 14
AF / HCP
SC / SF
F
Thermal effect of competing order
Magnetic resonance mode; rotons

## Slide 15
AF
SC
La(O,F)FeAs
AF / HCP
SC / SF
F
(b)

## Slide 16
Nernst Effect and Photo-excited transient SC
-- Overcoming competing order --

## Slide 17
Vortex-like Nernst onset
N.P. Ong et al. 2000
Nernst Effect
Diamagnetic Susceptibility

## Slide 18
Andrea Cavalleri
Photo
excited

## Slide 19
boson
boson

## Slide 20
Effect of Photo Excitation
LBCO. LESCO: Melting Charge and Spin Stripe Order
Inducing transient Superconductivity
YBCO: Melting Resonance Mode (inelastic mode)
Inducing transient Superconductivity
Eliminating
Competing
State

## Slide 21
Anomalous disappearances of superfluid responses
in the overdoped region

## Slide 22
nhole
ns
ns/m*
nn
Overdoped Tl2201
Uemura Nature 1993
Niedermayer PRL 1993

## Slide 23
Fig. 7
(a)
(b)
(c)
(d)
CT
BCS

## Slide 24
Superfluid Density of Tri-layer Twisted Graphene
Philip Kim et al. Nature (2025)

## Slide 25
Twisted Tri-layer Graphene
YBa2Cu3Ox
La(O,F)FeAs

## Slide 26
Comparable spin and charge energies
Model of synchronizing spin and charge time scales
“ Traffic Light Resonance ”

## Slide 27
Moriya-Ueda
Tc ~ max (hwSF)
Tc ~ eF
eF ~ J
Spin Fluctuation Energy

## Slide 28
Spin Fluctuation Temperature TSF [K]
Charge energy scale eF
Spin energy scale J
CuO
FeAs
Heavy Fermions
eF = J
UPt3
URu2Si2
Ba122FeAs
YBCO123
Tl 2223
UPd2Al3

## Slide 29
x
x
x
hwAF ~ kTF
Dynamically avoiding frustration

## Slide 30
No frustration for Nodal Charge Motion
Antinodal Charge Needs Cooperation of AF fluctuations
Nodal Charge Does NOT Need that
Nodal Charge
 Coherent nodal charge

## Slide 31
Traffic-light resonance
How a charge (= car)
can avoid
spin selection rules, frustration and Hubbard U (= red traffic light)
J ~ hwAF ~ kTF
Static order prevents charge motion

## Slide 32
Charge energy eF
Spin energy J
Pairable charges

## Slide 33
Unconventional Superconductors
MuSR: superfluid charge energy scales
Neutron scattering: spin energy scales
 Combination reveals novel spin-charge quantum interplays