## Slide 1: Cooperative use of muons and neutrons to sleuth ‘hidden’ order in f-electron magnets
Gregory J. MacDougall
University of Illinois at Urbana-Champaign

## Slide 2: Muon spin rotation/relaxation (μSR)
Muon precession reflects the magnet field environment inside materials
Frequency Mean field
Amplitude Volume fraction
Relaxation Second moment
/Fluctuations

## Slide 3: Who uses μSR?
Variants of SR are making meaningful contributions to the areas of:
  Magnetism
  Superconductivity
  Molecular systems
  Quantum diffusion
  Hydrogen storage
  Battery materials
  Semiconductors
  Radical chemistry
  Thin films and heterostructures
User base of ISIS facility,
courtesy of A. Hillier

## Slide 4: The peculiar case of Ce2O3
T. Kolodiazhnyi et al., PRB 98, 054423 (2018)
A. Cote et al., arXiv 2303.11878 (2023)
H || c
H. Pinto et al., Phys. Lett. 88A, 81 (1982)
meff = 2.17 μB
Θ = 27.7 K
But no magnetic
Bragg peaks!
(morder < 0.3 μB)

## Slide 5: “Hidden order” problems
M.B. Maple et al., PRL 56, 185 (1986)
T.E. Mason et al., PRL 65, 3190 (1990)
m = 0.037 μB
Magnetic transition
Small moment
(must be itinerant)
Large jump in Cp
(not itinerant)
URu2Si2
Order is hidden!!
(from neutrons)

## Slide 6: “Hidden order” problems
M.B. Maple et al., PRL 56, 185 (1986)
T.E. Mason et al., PRL 65, 3190 (1990)
URu2Si2
Publications explicitly using the words “hidden order” in abstract
Materials of interest include heavy fermion metals, quantum spin systems, 2d materials, photonic crystals, and unconventional superconductors of many types. Compounds skew heavily to large-Z elements.
Progress has required the synergistic use of multiple probes on the same samples.
m = 0.037 μB

## Slide 7: μSR example: Phase separation in URu2Si2
M.B. Maple et al., PRL 56, 185 (1986)
T.E. Mason et al., PRL 65, 3190 (1990)
m = 0.037 μB
AF order is a competing phase, enhanced by pressure
G.M. Luke et al., Hyperfine Int. 85, 397-409 (1994)
H. Amitsuka et al., Physica B 326, 418-421 (2003)
N.P. Butch et al., PRB 82, 060408(R) (2010)

## Slide 8: μSR example: small moment order in ScV6Sn6
Z. Guguchia et al., Nature Communications 14: 7796 (2023).
H.W. Suriya Arachchige et al., PRL 129 216402 (2022).
F. Grandi et al., PRB 107, 155131 (2023)
Time reversal symmetry breaking field consistent with predicted loop current order!
~1G

## Slide 9: μSR example: small moment order in the cuprates
C.M. Varma, PRB 73, 155113 (2006)
G.J. MacDougall et al., PRL 101, 017001 (2008)
B. Fauqué et al., PRL 96, 197001 (2006)
YBa2Cu3O7-δ
La2-xSrxCuO4
m = 0.1 μB
Hpredicted = 40G
Hmax = 0.2G
Loop current order must be dynamic (ν > 400MHz) if it is present !

## Slide 10: μSR example: Multipole order in NpO2
Neutron scattering limit mdipole < 0.01 μB
P. Santini and G. Amoretti, PRL 85, 2188 (2000)
W. Kopmann et al., J. Alloys and Compounds 271-273, 463-466 (1998)
m = 0.1 μB
D.W.. Osborne and E.F. Westrum,
J Chem. Phys. 21, 1884 (1953)
Consistent with
ordering of octupoles!
M.D. Frontzek et al., J. Solid State hem. 321, 123875 (2023)

## Slide 11: Reminder: origin of multipoles
https://ecampusontario.pressbooks.pub/enhancedchemistry/
3d materials
HCEF ~1000 – 5000 meV
HSO ~ 6 – 125 meV
H = HCoulomb + HCEF + HSO
Single ion Hamiltonian
4f materials
HCEF ~ 10 – 100 meV
HSO ~ 100 – 500 meV
L = 0
L = 1
L = 2
L = 3
HSO = λ L▪S
HCEF =
and equivalents

## Slide 12: Crystal field example: MgEr2Se4
D. Rieg-i-Plessis e al., PRB 89, 134438 (2019)
and
95%
axial
5%
transverse

## Slide 13: Sleuthing hidden order in Ce2O3
Step 1: Neutron powder diffraction
BT-1
T = 2 K
POWGEN
T = 2 K
Results
Confirm (twice) that there is no magnetic Bragg peaks below T* = 6.5 K
Place upper limits on any ordered moment that could exist and not be detected:
A. Cote et al., arXiv:2303.11878
G. Sala et al., PRMaterials 2, 114407 (2018)
m < 0.3 μB
m < 0.026 μB
Also confirm that there are no observable structural distortions at T* !

## Slide 14: Sleuthing hidden order in Ce2O3
Results
ZF-μSR spectra reveal an emergent TRSB field below T* of f = 14 MHz → 1 kG at the muon site.
A. Cote et al., arXiv:2303.11878
Step 2: μSR
(c.f. mND < 0.026 μB)
(c.f. mND < 0.3 μB )
m = 2.45-2.65 μB
m = 0.4 μB
LAMPF
1kG
Rapid of LF-μSR indicates ordered state is static on the μs timescale.
Muon stopping sites were calculated using the MuFinder software suite and ordered moment sizes were extracted from the TRSB field, assuming purely dipolar spins.

## Slide 15: Sleuthing hidden order in Ce2O3
Step 3: Inelastic neutron scattering
A. Cote et al., arXiv:2303.11878
Merlin
Ei=160meV
T=10K
Ei=12 meV
T=2K
Results
TOF neutron spectrometry with multiple Ei revealed two CEF excitations, which were fit to extract parameters for Ce3+.
Dormant multipolar degrees of freedom
Multipole | Channel | Operator | Moment
Dipole | axial | g¦¦ | 0.24
 | transverse | g | 2.26
Quadrupole | axial |  | -5.85
 | transverse |  | 1.96
Octupole | axial |  | 1.31
 | transverse |  | 4.84
Multipole | Channel | Operator | Moment
Dipole | axial | g¦¦ | 0.24
 | transverse | g | 2.26
Quadrupole | axial |  | -5.85
 | transverse |  | 1.96
Octupole | axial |  | 1.31
 | transverse |  | 4.84
rigid
A dispersive collective excitation was also observed at T=2K consistent with dipoles
Associated wavefunctions provide complete information about the multipolar matrix elements of the effective spin system:

## Slide 16: Sleuthing hidden order in Ce2O3
Step 3: Inelastic neutron scattering

## Slide 17: Sleuthing hidden order in Ce2O3
Step 4: Get to sleuthing
Ei=12 meV
T=2K
No structural distortion  the primary OP is not quadrupolar order
TRSB field seen with μSR  large moment from odd-rank tensor (dipoles, octupoles,..)
Neutron diffraction  ordered dipole moment is small
Emergent magnon  excitations are dipole-like
Octupoles can explain everything. Two possibilities:
  Ordering of axial octupoles
    Sympathetic order of weak (g|| = 0.24) axial dipoles
    Excitations tap much larger (g = 2.26) transverse dipoles, hybridized with octupoles
    Axial quadrupole is rigid and leaves lattice unaffected
  Ordering of transverse octupoles
    Coherent superpositions of Kramers states forces the dipole moment to zero
    Large in-plane dipole still accessible dynamically, leading to dipole like excitations
    Secondary coupling to transverse quadrupoles (, completely explain the anomaly in the dielectric constant through critical fluctuations of the octupolar order parameter.
Neutron spectroscopy  Magnetic moments have significant dipole, quadrupole and octupole contributions. What is ordering?

## Slide 18: Final thoughts: why care about multipoles?
Multipoles are hard to and understanding requires synergistic investigation with multiple techniques
 There is a clear and immediate benefit from co-locating neutron and muon sources
Energy scales in rare-earth (4f) and actinide (5f) materials are dominated by spin-orbit coupling,  all electron orbits are magnetic and all magnetic moments have significant multipolar character.
https://www.stanfordmagnets.com/a-comprehensive-overview-of-rare-earth-magnets.html
  Several avenues are being explored that make use of multipolar degrees-of-freedom:
  e.g. -densely packed, non-volatile memory with ultrafast (THz) switching capability
  - precision magnetoelectrical sensors controllable with compact electric fields
      -isolated quantum information (qubit) storage
  - multipolar-mediated superconductors with topologically protected edge states
Rare-earth elements dominate (~70%) the magnetic materials market (~$35-60 billion), which is growing at a CAGR of ~8%.
And contribute prominently to emerging fields like spintronics ($1.7-3 billion) and quantum information ($1.5-3.5 billion), each projected to grow at rates as high as 35% CAGR.

## Slide 19: SEEMS: a next generation muon source
Review of Scientific Instruments 94, 033908 (2023)